Add : 522-2, Yongseong-Ri, Samseong-Myeon, Eumseong-Gun, Chungcheongbuk-Do, Korea

Tel : 82-43-879-8835  Fax : 82-43-879-8839

Homepage : www.welcron.com

Data Sheet

|  | Mechanical Properties | Unit | Spec | Result |
| --- | --- | --- | --- | --- |
| 1 | Material | - | PP 100% Melt Blown |
| 2 | Basis Weight | GSM | 30 ± 15% | AVG. 28.3 |
| 3 | Efficiency of Filtration | % | 98↑ | AVG. 99.536% (99.511, 99.482, 99.527, 99.510, 99.617, 99.573) |
| 4 | Pressure Drop | mmAq | 15.0↓ | 8.4 |
| 5 | width | mm | Max 1,500 |

Item : MF0030FS(N-95)                      Date : 15th November 2017

Note) 1) Test Method of Efficiency of Filtration and Pressure Drop

- Measurement Instrument : TSI 8130

- Flow Rate : 85LPM

- Particle Size : 0.3 micron

- Test Particle : NaCl